Sample Specification 1100HV

Restraint for existing bell joints found on

C905 PVC pipes shall consist of the

following: The restraints shall be

manufactured of ductile iron conforming to

ASTM A536. The split restraint rings,

incorporating a plurality of individually -

actuating gripping surfaces, shall be used to

grip the pipe on either side of the bell. A

sufficient number of tie bars casted from

ASTM A536 shall be used to span the

distance between the restraints and a

sufficient number of bolts shall be used to connect each

restraint to the tie bars. The restraint devices

shall be coated using MEGA-BOND™. (For

complete specifications on MEGA-BOND visit

www.ebaa.com.) The combination shall have

a minimum working pressure rating as

shown in the adjacent table. The restraint

shall be the Series 1100HV, as manufactured

by EBAA Iron, Inc., or approved equal.