Restraint for mechanical joints shall consist of the following: The restraint shall be manufactured of ductile iron conforming to ASTM A536. The restraint devices shall be coated using MEGA-BOND. (For complete specifications on MEGA-BOND visit www.ebaa.com.) The screws shall have a Rockwell hardness of C40-45 converted from Brinnell. The gland shall have a design to fit standard mechanical joints with standard T head bolts conforming to ANSI/AWWA C111/A21.11 and ANSI/AWWA C153/A21.53 of latest revision. The combination shall have a working pressure as shown in the adjacent table. The restraint shall be the Series 1200, as manufactured by EBAA Iron, Inc, or approved equal.